1. 报告题目：

Local Environments and Molecular Engineering of Semiconductor Nanocrystals

(半导体纳米颗粒的微观环境及其分子工程)

2. 报告摘要：

- 半导体纳米颗粒(量子点)具有优异的光电性质,其发光在可见和近红外随尺寸简单可控。其在生物成像，发光器件，太阳能电池，光电探测器和量子计算上有广泛应用。量子点的微观表征与修饰，及相应的分子甚至原子工程是材料科学中最有趣的研究课题之一。在本研究中我们开发了一个磁性探针，可以灵敏探测量子点表面和核的微观环境，以及核/壳量子点的界面环境。在纳米颗粒内部进行掺杂可以有效改善其性质以实现多功能纳米材料。报告人开展了掺杂量子点的光学性能的调控及在发光器件和绿色能源的应用研究。在纳米颗粒的表面，我们采用脂质囊泡包裹的方法，有效的将疏水性量子点转移到水溶液。试验和理论研究表明脂膜的物相可以控制量子点的物理和化学性质。据此我们得到了水溶液中最光稳定的简单量子点。同时用磷脂囊泡模板和DNA碱基配我们成功的对量子点的特殊位点进行表面修饰和分子工程。由此得到的多功能纳米结构可以用于生物环境中的荧光成像和潜在药物传递。

- 附英文摘要：

- Semiconductor nanocrystals or named quantum dots (QDs) with unique dimension-dependent electric and optical properties are one of the most interesting materials capturing the interest of researchers over the past decades, and have broad applications in biological imaging, light-emitting devices, solar cells, photo-detectors, and quantum computing. In my study, a sensitive magnetic probe was developed to detect the microenvironments of surface and core of a QD, as well as interface of core/shell QDs. Doping inside the nanocrystals is an important method to manipulate the properties with the aim of multifunctional nanomaterials. We have used dopants to fine turn the optical properties of the nanomaterials. Surface modification such as lipid vesicle encapsulation is an efficient approach to transfer hydrophobic QDs into aqueous solutions. Our study indicates that lipid membranes can control the chemical and optical properties of QDs in a phase-dependent manner. Using gel-phase lipid vesicle templates, we are able to achieve the most photostable non-core/shell QDs in aqueous solution. More importantly, the site-specifically engineering of QDs can be achieved using phospholipid-QD hybrid vesicle templates to generate gold NP-QD assemblies programmed by Watson-Crick base-pairing for use as a multi-functional cargo for fluorescence-based imaging and potential drug delivery.

3. 个人简介：

- 郑伟威博士，2005年于中国科学技术大学获理学硕士学位，硕士期间主要从事水热合成宽带隙半导体晶体方面的研究。2005年至2011年在美国佛罗里达州立大学化学与生物化学系从事稀磁半导体量子点的磁性与量子点尺寸和掺杂位置关系研究，获博士学位。2012年至2015年，在美国埃默里大学从事量子点的功能化及在生物体系中的应用研究。2015年至今任职副教授于美国雪城大学化学系， 并开展纳米材料在绿色能源方面应用的研究。其在水相体系获得了光学上最稳定的非核壳结构的量子点，并通过脂质体胶体模板实现了特定位置的选择性功能化；首次报道了Cr掺杂的ZnSe量子点，并发现了ZnSe量子点核中存在具有尖晶石结构的ZnCr2Se4包容物；在Mn掺杂的II-VI量子点中发现了表面载流子调制的铁磁耦合以及Cr掺杂的II-VI量子点中的相转化现象；发展了一种灵敏的磁性探针，可用于检测量子点的表面、核及界面的微环境及晶格应力。相关研究分别发表在J. Am. Chem. Soc.、Nano. Lett. 、Adv. Funct. Mater. 及J. Phys. Chem. C 等杂志上。郑伟威博士的研究曾获得美国佛罗里达州立大学的最佳博士学位论文奖。

4. 代表性论文（限一作或通讯作者论文，不超过5篇）：

参考格式：

- Zheng, W.; Yang, L. West, A.; Schuler, E.; Yehl, K.; Kindt, J. T.; Salaita, K. Quantum Dots Encapsulated within Phospholipid Membranes: Phase-dependent Structure, Photostability, and Site-selective Functionalization. J. Am. Chem. Soc. 2014, 136, 1992-1999.

- Zheng, W.; Wang, Z.; van Tol, J.; Dalal, N. S.; Strouse, G. F. Alloy Formation at the Tetrapod Core/Arm Interface. Nano. Lett. 2012, 12, 3132–3137.

- Zheng, W.; Kumar, P.; Washington, A,; Wang, Z.; Dalal, N. S.; Strouse, G. F.; Singh, K. Quantum Phase Transition from Superparamagnetic to Quantum Superparamagnetic State in Ultrasmall Cd1-xCr(II)xSe Quantum Dots? J. Am. Chem. Soc. 2012, 134, 2172–2179.

- Zheng, W.; Singh, K.; Wang, Z.; Wright, J. T.; van Tol, J.; Dalal, N. S.; Meulenberg, R. W.; Strouse, G. F. Evidence of a ZnCr2Se4 Spinel Inclusion at the Core of a Cr Doped ZnSe Quantum Dot. J. Am. Chem. Soc. 2012, 134, 5577–5585.

- Zheng, W.; Strouse, G. F. Involvement of Carriers in the Size-dependent Magnetic Exchange for Mn:CdSe Quantum Dots. J. Am. Chem. Soc. 2011, 133, 7482–7489.